## Slide 1
Fig. 1
Immediate and Cycling
Overpotential
Epa
1 mM
Fe(NO3)3
1 mM Fe(NO3)3
e- per Ni
Ni1-z FezOxHy
z (%) =
0 %
0
11
16
21
z (%) =
11 %
16 %
24 %
A
B
C
24
Cycle #
21 %
Notes: Fixed – this is 4p235 data (Fe-spiked)
Talk about similar loading...

## Slide 2
Figure 2
Ni-Fe conductivity
1 mM
Fe(NO3)3
(2)
Pre- Fe
(1)
(3)

## Slide 3
Fig. 3 Co-dep vs spiking
30 %
25%
0%
Co-deposited
Spike
B
C
A
8 %
10 %
0%
Fe (%)
Co-deposited
Spike
D
Open = co-deposited
Closed = spiked
Fe (%)
Open = co-deposited
Closed = spiked

## Slide 4
Supplementary Information

## Slide 5
Figure S1
CV 5-104
CV 4
NiOxHy
e- per Ni
Epa
A
B
C
D
E
Ni 2p
Fe 2p

## Slide 6
Figure S2
Anodic
Cathodic
0 %
1 mM Fe(NO3)3
Ni1-zFezOxHy
B
D
C
1 mM Fe(NO3)3
0 %
Ni1-zFezOxHy
2nd peak
Anodic
Cathodic
CV =
4
5
14
34
104
A
2nd peak

## Slide 7
Figure S3
Get Ni-only conductivity here….
(2)
(1)
(3)
NiOxHy

## Slide 8
Figure S4
Fe-Free
base
1 mM Fe(NO3)3
NiOxHy
NiOxHy
Pt
Pt
Fe-spiked on Ni w/Au and Pt substrate
ROLE of substrate
Fe-Free
base
1 mM Fe(NO3)3
NiOxHy
NiOxHy
Au
Au
A
B

## Slide 9
Figure S5
SEM
A
B
C
D

## Slide 10
Ni
Fe
Fe
Ni
Fe
Ni
Ni

## Slide 11
Ni
Fe
Fe
Ni
Fe
Ni
Ni

## Slide 12
Figure
XPS vs ICP composition
Open = co-deposited
Closed = spiked
Notes: Change for Ni that was cycled differently.... Could you say that the Fe is not evenly distributed with this data?

## Slide 13
Ni
Fe
Ni
Fe
Ni
Notes: Change for Ni that was cycled differently.... Could you say that the Fe is not evenly distributed with this data?

## Slide 14
Figure
XPS/ICP
composition
A
0 %
6 %
10 %
20 %
25 %
Co-dep
Fe spike
100 CV
10 CV
2 CV
Ni 2p
Fe 2p
6 %
10 %
20 %
25 %
Notes: Remove the 0% from old one and add new...need to change out 10 CV and add 30 CV as well and Co-dep Ni99Fe01 – add co-dep for different compositions? Add zero – figure out why Fe peaks appear to be shifting...

## Slide 15
Fe-free
edge/defect
bulk
Fe3+ added to electrolyte
NiOxHy
Notes: 3.25 by 1.75